**Technical Datasheet UV5**

**Product Description**

Bondchem UV5 is a single component, medium viscosity, ultra fast cure UV light curable structural adhesive. This grade is designed to bond medium to large surface area glass to glass applications. Once cured this grade offers optimum clarity and excellent environmental resistance.

**Typical Applications**

Bondchem UV5 cures in seconds upon exposure to UV light to form an impact resistant flexible bond. It is used widely on many substrates and applications in both industrial and medical market sectors. Typical applications shown below:

* Bonding glass bevel assemblies.
* Laminating glass.

**Instructions For Use**

This adhesive is UV sensitive, any exposure to daylight, UV light and artificial light should be kept to an absolute minimum during storage and handling.

1. Clean parts fully and apply adhesive to one of the mating parts.
2. Assemble parts, and position ensuring any bubbles are removed prior to cure.
3. Apply UV light and allow to cure.\*
4. As the cure rate depends upon lamp intensity, distance from light source, depth of cure needed, bondline gap, and the light transmittance through the substrate itself, it is always advisable to test and assess cure speed prior to production.
5. For guidance, if the gel time under UV exposure = **X** always allow a minimum of **X+2X** for a full cure before moving the parts.

\*Cure rate depends upon lamp intensity, distance from light source, depth of cure needed, bondline gap, and the light transmittance throught the substrate itself.

**Properties of Uncured Material**

|  |  |
| --- | --- |
| Resin | Urethane Acrylate |
| Appearance | Clear Liquid |
| Viscosity | 1750cps |
| Cure System | UV |

**Performance of Cured Material**

|  |  |
| --- | --- |
| Cure speed glass to glass | <10 Seconds |
| Typical bond Strength | 15 - 20Nmm2 |

**Packaging**

Bondchem UV5 is available in 200g black bottles.

**Storage & Shelflife**

Bondchem UV5 should be stored unopened in a cool dry location, out of direct sunlight. Stored correctly , this grade can offer a 12 month shelf life from manufacture.

**Health and Safety in Use**

**Bondchem UV5 should not be used without consulting the MSDS, which contains full information regarding the use of this product, including Transport, Disposal, Toxicological, Exposure Controls, Accidental Release and First Aid measures essential to the safe use of this product.**