Technical Datasheet

Holdtite CA46

Product Description

Holdtite CA46 is an advanced, low odour, low bloom cyanoacrylate that is formulated to provide high tensile and shear strengths on a wide variety of substrates. This single component adhesive has an active cure mechanism, which when pressed into a thin film between two surfaces, will cure almost instantaneously to form a rigid thermoplastic. Due to the innovative chemistry of CA46, this grade eliminates blooming, even when cured in volume.

Typical Applications

Holdtite CA46 is used in a huge cross section of industrial applications. From OEM to MRO industries, this grade can be used on a variety of plastic, rubber and metal bonding applications including automotive and electronic component manufacturing. Typical examples shown below:

- Bonding ABS and stainless steel on automotive center consoles

- Bonding sensors on PCM’s

- Bonding polycarbonate and acrylic in POS displays

- Bonding components in a speaker cone

- Bonding protective screens to casing in TV manufacture

- Bonding plastic lenses in traffic lights

Instructions For Use

- For best results clean all surfaces with a cleaning solvent and allow to dry fully.

- Apply adhesive to one of the mating parts and assemble carefully.

- Allow to cure fully before applying load.

- Excess adhesive can be carefully cleaned up with cleaning solvents such as acetone.

Properties of Uncured Material

| Resin | Methoxyethyl Cyanoacrylate |
| --- | --- |
| Appearance | Colourless liquid |
| Viscosity | 40 to 80cps |
| Cure System | Humidity |

Performance of Cured Material

| Fixture Speed | < 30 seconds @ 20°C |
| --- | --- |
| Full Cure Time | 24 hours @ 20°C |
| Typical Strength | 5 to 28 N/mm2 |
| Gap Fill | 0.1mm |
| Temperature Range | -55°C to 70°C |

Packaging

Holdtite CA46 is available in 3g, 20g, 50g and 500g HDPE bottles. In addition, we can offer automated dispensing lines for the bulk dispensing of this material.

Storage & Shelflife

Holdtite CA46 should be stored unopened in a cool dry location, out of direct sunlight. Stored correctly , this grade can offer a 6 month shelf life from manufacture.

Health and Safety in Use

Holdtite CA46 is an ethyl cyanoacrylate, and can bond skin and eyelids in seconds. This grade should not be used without consulting the MSDS, which contains full information regarding the use of this product, including Transport, Disposal, Toxicological, Exposure Controls, Accidental Release and First Aid measures essential to the safe use of this product.

The data, information and values contained in this Technical Data Sheet have been obtained by specific tests conducted in a controlled environment, and should be used for guidance purposes only. Although we believe them to be reliable and accurate, users should always conduct their own tests in their specific working conditions to ensure that the product is suitable and effective for use. It is the users sole responsibility to determine the suitability of the product for the application. Bondchem Ltd cannot be held responsible for the results of procedures undertaken elsewhere, nor for the safeguarding of personnel or property, all of which is the duty of the user. Suitability of products or methods is discretionary. Therefore, warrantees or implied usage obligations should not be attributed to, and are not the responsibility of, Bondchem Ltd. Bondchem Ltd are not liable for any financial loss or other damages incurred by the user as a result of the use of this product.